E0900131-v2

35 Watt Air Cooled  Beam Dump Assembly procedures

D0900177 and D090095

D0900345 Si –Substrate Mounting Procedure

- Clean the si-Mirror and Heat Sink body with alcohol before bonding.

- Mix the Silver epoxy [ McMaster part 7595A33] one to one.

- Apply to the backside of the si-Mirror, spread a layer .005”-010” thick, using a razor blade.

- Press the si-Mirror and Heat Sink together and let the parts cure for 24 hours at room temperature.

D090095 Beam Dump General Assembly Instructions.

- Attach  the feet to the Heat Sink body,  as shown in the drawing,

- Put two Part 17 washers between the part 10 bracket and the part 1 Heat Sink body typ.

- Push Part 5 & 22 against the heat sink body flange as shown so there is no gap.

- Part 16 to contact Part 5 & 22, check the orientation of the drill point feature, and tighten the top and bottom 4-40 button hd. screws.

D0900177 Beam Dump General Assembly Instructions.

- Attach the feet to the Heat Sink body, as shown in the drawing.

- Push part 5 & 4 against the heat sink body flange as shown so there is no gap.

- The longer part of the foot part D0900809 should be forward as shown.

- Part 12 to contact Part 5 & 4, check the orientation of the drill point feature, and tighten the top and bottom 4-40 button hd. screws.

D0900177 and D090095 Beam Alignment Procedure

- There are two target tools (D0900843 & D0900901 ) one with a mirror, and one with a center hole.

- Target D0900843 is used to center the beam (step 1), then is replaced with the mirror D0900901 to retro reflect the beam back on itself (step 2).

- In Beam Dump D090095, the part D0900814 should be clamped to pivot the entire assembly about the shoulder screw which is centered at the aperture opening.

- The D0900177 will need to have step (step 2) done manually after the beam is first centered in the aperture hole with target D0900843