| AUTHOR: | CHECKED: | DATE | APPROVALS |
| --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley | Coyne | 6-16-06 | E060179-00 | A |  |

Applicable Documents

LIGO-D040431-B	Quad ETM Silica Test Mass
LIGO-D030265-A	Fused Silica Blank LASTI Test Mass
LIGO-E030309-A	Fused Silica Blank, LASTI Test Mass, R&D
LIGO-E050191-A	Shape and Polish LASTI ETM Blank

MIL-PRF-13830B	General Specification Governing the Manufacture, Assembly, and Inspection of 
Optical Components for Fire Control Instruments

Requirements

Physical Configuration

According to
LIGO-D040431	Quad ETM Silica Test Mass, X dimension 200.0 ± 0.5 inches

Fabricate from
LIGO-E050191	Shape and Polish LASTI ETM blank
LIGO-E030309	Fused Silica Blank, LASTI Test Mass, R&D

Optical Surface Figure, Sides 1 and 2 - FLAT.  Measured over the central 120 mm diameter

Surface 1:  Flat to /10 peak to valley, measured at 633 nm
Radius of curvature: >150 km

Surface 2:  Flat to /10 measured at 633 nm
Radius of curvature: > ±20 km

Surface Error, High Spatial Frequency:  “microroughness”
measured over the central 120 mm diameter

Surface 1 HSF error rms < 0.2 nanometers

Surface 2 : not specified

Scratches, Sleeks and Point defects

Scratches, sleeks and point defects are evaluated according to MIL-PRF-13830B

Side 1

Within the central 20mm diameter:  10/5
Within the central 120 mm diameter:  20/10
Outside the central 120 mm diameter:  40/20

Side 2

Within the central 120 mm diameter:  40/20

Inspection

- Inspections

| Specification | Test Method | Data Delivered |
| --- | --- | --- |
| Scratches and Point defects, side one | Visual Inspection | Certification |
| Figure, side one | Interferometry | Surface phase map |
| Surface Errors - High Spatial frequency, side one | Interferometry | Surface maps for 3 central locations. Numerical values included with certification |

Orientation:  For the purpose of phase maps the substrate shall be oriented such that the point of minimum thickness shall be at the top center of the data.

# Comments

150Km = 30 nm sag over 200 mm diameter

This ~l/10 requirement should yield ~10nm rms/120mm diameter, & much better over LASTI beam diameter (~1cm)

20Km = 250 nm sag over 200mm diameter

General Optics

“commercial” = 20/10

“research” = 10/5

"Utility" = 40/20