| AUTHOR: | CHECKED: | DATE | APPROVALS |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley | Coyne | 6-16-06 | E060179-00 | A | 6-26-06 |
| G. Billingsley |  | 8-18-06 | E060183-00 | B |  |

Applicable Documents

LIGO-D040431-C	Quad ETM Silica Test Mass
LIGO-D030265-A	Fused Silica Blank LASTI Test Mass
LIGO-E030309-A	Fused Silica Blank, LASTI Test Mass, R&D
LIGO-E050191-A	Shape and Polish LASTI ETM Blank

MIL-PRF-13830B	General Specification Governing the Manufacture, Assembly, and Inspection of 
Optical Components for Fire Control Instruments

Requirements

Physical Configuration

According to
LIGO-D040431	Quad ETM Silica Test Mass, X dimension 200.0 ± 0.5 millimeters

Fabricate from
LIGO-E050191	Shape and Polish LASTI ETM blank
LIGO-E030309	Fused Silica Blank, LASTI Test Mass, R&D

Optical Surface Figure, Sides 1 and 2 - FLAT.  Measured over the central 120 mm diameter

Surface 1:  Flat to < /10 Peak to Valley, measured at 633 nm

Surface 2:  Flat to < /3 Peak to Valley, measured at 633 nm

Surface Error, High Spatial Frequency:  “microroughness”
measured over the central 120 mm diameter

Surface 1 HSF error rms < 0.2 nanometers

Surface 2 : not specified

Scratches, Sleeks and Point defects

Scratches, sleeks and point defects are evaluated according to MIL-PRF-13830B

Side 1

Within the central 20mm diameter:  10/5
Within the central 120 mm diameter:  20/10
Outside the central 120 mm diameter:  40/20

Side 2

Within the central 120 mm diameter:  40/20

Inspection

- Inspections

| Specification | Test Method | Data Delivered |
| --- | --- | --- |
| Scratches and Point defects, side one | Visual Inspection | Certification |
| Figure, side one | Interferometry | Surface phase map |
| Surface Errors - High Spatial frequency, side one | Interferometry | Surface maps for 3 central locations. Numerical values included with certification |

Orientation:  For the purpose of phase maps the substrate shall be oriented such that the point of minimum thickness shall be at the top center of the data.