| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Name Jeff Kissel | Name Ken Mason | 617-324-5250 | Enhanced LIGO HAM SEI |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D071006-01 D071006-02 |  | stage 0 stiffener rib, AL 6061 stage 0 stiffener rib, AL 6061 |  | 2 1 |

| Used In (next higher assembly): |  |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |
| HPD |  |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean | 12/20/07 | LLO | clean per LIGO E960022, clean in Liquinox for 10 minutes. Rinse in distilled water at least 3 times, changing the rinse water every time. Ultrasonic clean in methanol for 10 minutes. | T.E. | 12/20/07 |
| 2 | Vacuum Bake | 1/2/08 | LLO | bake per E960022—because of size will need to be air baked and FTIR’d. Items fit in LLO VBO | T.E. | 1/5/08 |
| 3 | Control Point | 1/5/08 | LLO | Review/Approve RGA scan | BO’R | 1/7/08 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.E. | 1/7/08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: stays at LLO, c/o Ken Mason File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 1/17/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

These plates are for the enhanced LIGO HAM SEI installation at Livingston. They will be needed by mid to late November 2007.