| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Adam Mullavey | J. Romie | 225 686-3160 | OMC, ELIGO |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D070177 | 00 | Tip Tilt Suspension Bars – Stainless Steel | SN 001/002 | 2 |

| Used In (next higher assembly): | OMC |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |
| N |  |  |  |  |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | Per LIGO E960022: -Ultrasonic clean in Liquinox for 10 minutes. -Rinse in distilled water at least 3 times, changing the rinse water every time. | T.E. | 3-6-08 |
| 2 | Vacuum Bake |  |  | Per E960022, Class A, 200ºC for 48 hours | T.E. | 3-10-08 |
| 3 | Control Point |  |  | Review/Approve RGA scan | BO’R | 3-11-08 |
| 4 | Wrap and Tag vacuum clean parts |  |  |  | T.E. | 3-11-08 |
| 5 | Ship and Deliver/File paperwork |  |  | To be used at LLO site. No shipping required. | BO’R | 4-21-08 |