| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: L. BARSOTTI | 12-15-2010 |  |  |  |  |  |  |
| CHECKED: |  |  |  |  |  |  |  |
| APPROVED: P.FRITSCHEL |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

# Description

Super-polished fused silica lenses, AR/AR coated for 1064nm and 532nm

# Material

Corning 7980-0F

# Surface Roughness

Side 1

Super polish

Surface Roughness: <2Å RMS in CA

Surface Quality: 10-5

Side 2

Super polish

Surface Roughness: <2Å RMS in CA

Surface Quality: 10-5

# Surface Figure

Side 1

Flat < λ/10 at 632.8 over central 80%

Side 2

Flat < λ/10 at 632.8 over central 80%

# Coating

Side 1 and Side 2

AR coating/0º (IBS)

R< 0.1% @ 1064nm

R<0.2% @ 532nm

# ROC and focal length

# E1000845-v1–01 PCX

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=+75mm ± 1%

Focal length (@1064nm) = +166.8mm ± 2%

Focal length (@532nm) = +162.8mm ± 2%

# E1000845-v1–02 PCX

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=+100mm ± 1%

Focal length (@1064nm) = +222.4mm ± 2%

Focal length (@532nm) = +217.1mm ± 2%

# E1000845-v1–03 PCX

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=+150mm ± 1%

Focal length (@1064nm) = +333.6mm ± 2%

Focal length (@532nm) = +325.6mm ± 2

# E1000845-v1–04 PCX

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=+200mm ± 1%

Focal length (@1064nm) = +444.8mm ± 2%

Focal length (@532nm) = +434.1mm ± 2%

# E1000845-v1–05 PCC

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=-25mm ± 1%

Focal length (@1064nm) = -55.6mm ± 2%

Focal length (@532nm) = -54.3mm ± 2%

# E1000845-v1–06 PCC

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=-38mm ± 1%

Focal length (@1064nm) = -84.5mm ± 2%

Focal length (@532nm) = -82.5mm ± 2%

# E1000845-v1–07 PCC

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=-50mm ± 1%

Focal length (@1064nm) = -111.2mm ± 2%

Focal length (@532nm) = -108.5mm ± 2%

# E1000845-v1–08 PCC

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=-75mm ± 1%

Focal length (@1064nm) = -166.8mm ± 2%

Focal length (@532nm) = -162.8mm ± 2%

# E1000845-v1–09 PCC

25mm +0.0/-0.1mm Ø X 6.35mm ± 0.1mm tk. (edge), ROC=-150mm ± 1%

Focal length (@1064nm) = -333.6mm ± 2%

Focal length (@532nm) = -325.6mm ± 2%

# E1000845-v1–10 PCC

50.8mm +0.0/-0.1mm Ø X 9.5mm ± 0.1mm tk. (edge), ROC=+150mm ± 1%

Focal length (@1064nm) = +333.6mm ± 2%

Focal length (@532nm) = +325.6mm ± 2%

# E1000845-v1–11 PCC

50.8mm +0.0/-0.1mm Ø X 6.4mm ± 0.1mm tk. (edge), ROC=+154.5mm ± 1%

Focal length (@1064nm) = +343.6mm ± 2%

Focal length (@532nm) = +335.4mm ± 2%

Serial numbers and registration marks shall be scribed or	etched on the barrel of	the optic for in-vacuum use. An arrow should point to the curved surface.

# Coating vendor to provide:

  - 1. Three spectrophotometer graphs of the reflectance of the AR coatings; one covering the spectrum from 300nm to 1200nm; the other two, with increased sensitivity, showing wavelengths from 450nm to 650nm and  900nm to 1100nm

            - 2. Spectrophotometer graphs of the reflectance of the AR coating taken as cited above.