LIGO Laboratory / LIGO Scientific Collaboration

LIGO- T1100056-v2	LIGO	4/4/11

Arm Cavity Baffle Edge Scatter

Michael Smith

Distribution of this document:

LIGO Scientific Collaboration

This is an internal working note

of the LIGO Laboratory.

| California Institute of Technology LIGO Project – MS 18-34 1200 E. California Blvd. Pasadena, CA 91125 Phone (626) 395-2129 Fax (626) 304-9834 E-mail: info@ligo.caltech.edu | Massachusetts Institute of Technology LIGO Project – NW22-295 185 Albany St Cambridge, MA 02139 Phone (617) 253-4824 Fax (617) 253-7014 E-mail: info@ligo.mit.edu |
| --- | --- |
| LIGO Hanford Observatory P.O. Box 159 Richland WA 99352 Phone 509-372-8106 Fax 509-372-8137 | LIGO Livingston Observatory P.O. Box 940 Livingston, LA 70754 Phone 225-686-3100 Fax 225-686-7189 |

http://www.ligo.caltech.edu/

1	Introduction	5

2	Scattering Theory	5

2.1	Parametric BRDF Function	8

2.2	Scattered Power into IFO	9

3	Results	12

3.1	Measured BRDF	12

3.1.1	Porcelainized Steel @ 3 Degree Incidence Angle	12

3.1.2	Oxidized Polished Stainless Steel @ 3 Degree Incidence Angle	13

3.2	Scattered Light Calculations	18

3.2.1	Baffle Irradiance	18

3.2.2	Power Scattered into IFO Mode from Baffle Plate Edge	19

3.2.3	Power Scattered into IFO Mode from Baffle Plate Bend	19

3.2.4	Total Power Scattered into IFO Mode from Baffle Plate Edge, Bend, and the Louver Surfaces of the ACB	20

3.2.5	Displacement Noise Due to Total ACB Scatter	21

3.2.5.1	Porcelainized Steel Scatter Noise	21

3.2.5.2	Oxidized Polished Stainless Steel Scatter Noise	22

Table of Figures

Figure 1:Light from the far mirror scatters from the ACB edge back into the IFO mode	5

Figure 2: ACB is tilted to reduce the back scatter	6

Figure 3: Geometry of the scattering calculation for the baffle plate edge	7

Figure 4: Geometry of the scattering calculation for the baffle bend	8

Figure 5: CASI Measurement of BRDF of Porcelainized Steel @ 3 Deg Incidence	12

Figure 6: Parametric Equation, Porcelainized Steel BRDF @ 3 deg Versus Scattering Angle Around the Specular Direction	13

Figure 7: CASI Measurement of BRDF of Porcelainized Steel @ 57 Deg Incidence	14

Figure 8: Parametric Equation, Porcelainized Steel BRDF @ 57 Deg Incidence Versus Scattering Angle Around the Specular Direction	15

Figure 9: CASI Measurement of BRDF of #4 Oxidized Polished Stainless Steel @ 3 Deg Incidence	16

Figure 10: Parametric Equation, #4 Oxidized Polished Stainless Steel @ 3 Deg Incidence BRDF Versus Scattering Angle Around the Specular Direction	17

Figure 11: Comparison of #4 Oxidized Polished SS and Porcelainized steel @ 3 Deg Incidence	18

Figure 12: Power Scattered into the IFO Mode from the Baffle Plate Edge, Porcelainized Steel	19

Figure 13: Power Scattered into the IFO Mode from the ACB Bend, Porcelainized Steel	20

Figure 14: Displacement Noise, Total ACB Scatter, Porcelainized Steel	21

Figure 15: Displacement Noise, Total ACB Scatter, Porcelainized Steel and Oxidized Polished Stainless Steel	23

Abstract

The scatter from the exposed frontal edges of the Arm Cavity Baffle is calculated. It depends upon the BRDF characteristics of the baffle material at small angles, upon the vertical tilt angle of the baffle edge, and upon the radius of the edge.

# Introduction

This document presents a calculation of the light scattered into the IFO arm cavity mode by the exposed vertical edges of the Arm Cavity Baffle.

The scatter from the exposed frontal edges of the Arm Cavity Baffle depends upon the BRDF characteristics of the baffle material at small angles, upon the vertical tilt angle of the baffle edge, and upon the radius of the edge.

# Scattering Theory

The primary source of scattered light from the Arm Cavity Baffle (ACB) is the small angle scatter from the COC mirror at the far end of the arm tube. This light will scatter from the edges and the bends of the ACB as shown in Figure 3 and Figure 4.

Figure 1:Light from the far mirror scatters from the ACB edge back into the IFO mode

Figure 2: ACB is tilted to reduce the back scatter

The incident angle at the baffle surface is θi , which depends upon  θxy , the angle of the normal to the surface,l and θt , the tilt angle.

The light must scatter by the angle 2θi ± θs in order to back-scatter into the incident beam direction.

Figure 3: Geometry of the scattering calculation for the baffle plate edge

Figure 4: Geometry of the scattering calculation for the baffle bend

## Parametric BRDF Function

The angular dependence of the BRDF of the ACB surface with respect to the incidence angle can be approximated by the following parametric expression. The parameters are adjusted to match the shape of the BRDF data as measured by the CASI scatterometer.

The estimated maximum value at normal incidence is BRDF0. The break-over angle, θ1 is the angle at which the BRDF0  value is half the maximum. The BRDF reaches a minimum constant value, BRDFθ2, for angles greater than the micro-roughness angle, θ2.

The slope modifier, β is chosen to match the slope of the measured BRDF function.

The micro-roughness constant, Cmr is chosen so that the BRDF is equal to the minimum value at large scattering angles.

micro-roughness constant

## Scattered Power into IFO

The light back-scattered into the interferometer mode from the incident beam power, dPi (θxy ) at an incident angle on the baffle surface θi is centered around the scatter angle 2θi . This light is scattered into the solid angle subtended by the area of the IFO mode divided by the (arm length)^2, and must be re-scattered by the surface of the COC mirror at the far end of the arm to enter the divergence cone of the IFO.

dPsIFO = dPi (θxy ) BRDFACB (2θi + θs ) (dAIFO /Larm2 ) BRDFCOC  ΔΩIFO

The incident power is equal to the incident radiant intensity, Ii , times the element of ACB scattering area.

dPi (θxy ) = Ii rHsin(θxy )d θxy

where r is the radius of the baffle edge and H is the vertical height of the baffle edge.

The element of area of the IFO  mode into which the light scatters is given by

dAIFO = 2[wIFO2 - (Larm θs )2 ]1/2

where   wIFO is the radius of the IFO mode.

The total power back-scattered into the IFO mode is calculated by integrating over the scattering angle and over all incident angles at the ACB scattering surface.

The integrated scattering function is given by.

The maximum incident angles for the bent baffle edge and for the plate edge are given below.

input angle range, bend, rad

input angle range, plate rad

The Baffle and IFO parameters used for the calculations are given below.

length of baffle plate edge, m

length of baffle bend edge, m

laser wavelength, m

IFO waist size, m

solid angle of IFO mode, sr

Transfer function @ 100 Hz, ITM HR

IFO arm length, m

Arm Power, W

radius of Cryopump aperture, m

half-angle from centerline to Rcp, rad

The scattering characteristics of the COC mirror is modeled with the following parametric function.

BRDF, sr^-1; CSIRO, surface 2, S/N 2

# Results

## Measured BRDF

The BRDF of porcelainized steel and oxidized polished stainless steel was measured with the CASI scatterometer. The scatterometer has a blind spot and cannot measure the maximum BRDF at the specular angle; therefore, the maximum BRDF and the break-over angle must be estimated by achieving the best fit of the data with the parametric equation. In the following, two sets of scatterometer data from different positions on the same sample, together with the instrument background signal and the best-fit parametric equation are shown. BRDF values are valid above the level of the instrument background signal, shown in the red trace.

### Porcelainized Steel @ 3 Degree Incidence Angle

The CASI BRDF data for two positions on a porcelainized steel sample @ 3 deg incidence is shown in Figure 5.

Figure 5: CASI Measurement of BRDF of Porcelainized Steel @ 3 Deg Incidence

Reflectivity of surface @ 3 deg incidence  	R = 0.02

Break-over angle                                    	θ1 = 0.9 deg

Micro roughness angle       			θ2 = 6 deg

Maximum BRDF0  				BRDF0	 = 50

Large angle BRDFla  				BRDFla = 0.035

Slope modifier 				β =2.7

Micro-roughness constant 			Cmr = 1186

The parametric equation with the best-fit to the scattering data is plotted in Figure 6.

Figure 6: Parametric Equation, Porcelainized Steel BRDF @ 3 deg Versus Scattering Angle Around the Specular Direction

### Porcelainized Steel @ 57 Degree Incidence Angle

The CASI BRDF data for two positions on a porcelainized steel sample @ 57 deg incidence is shown in Figure 7.

Figure 7: CASI Measurement of BRDF of Porcelainized Steel @ 57 Deg Incidence

Reflectivity of surface @ 57 deg incidence  	R = 0.001

Break-over angle                                    	θ1 = 0.5 deg

Micro roughness angle       			θ2 = 3.4 deg

Maximum BRDF0  				BRDF0	 = 10

Large angle BRDFla  				BRDFla = 0.04

Slope modifier 				β =2

Micro-roughness constant 			Cmr = 5439

The parametric equation with the best-fit to the scattering data is plotted in Figure 8.

Figure 8: Parametric Equation, Porcelainized Steel BRDF @ 57 Deg Incidence Versus Scattering Angle Around the Specular Direction

### Oxidized Polished Stainless Steel @ 3 Degree Incidence Angle

The CASI BRDF data for two positions on an oxidized polished stainless steel with four passes through the oxidizing furnace is shown in Figure 9.

Figure 9: CASI Measurement of BRDF of #4 Oxidized Polished Stainless Steel @ 3 Deg Incidence

Reflectivity of surface @ 3 deg incidence  	R = 0.02

Break-over angle                                    	θ1 = 1 deg

Micro roughness angle       			θ2 = 10 deg

Maximum BRDF0  				BRDF0	 = 6

Slope modifier 				β = 0.95

Micro-roughness constant 			Cmr = 3527

The parametric equation with the best-fit to the scattering data is plotted in Figure 10.

Figure 10: Parametric Equation, #4 Oxidized Polished Stainless Steel @ 3 Deg Incidence BRDF Versus Scattering Angle Around the Specular Direction

A comparison of the BRDFs for porcelainizing and oxidizing is shown in Figure 11.

Figure 11: Comparison of #4 Oxidized Polished SS and Porcelainized steel @ 3 Deg Incidence

## Scattered Light Calculations

### Baffle Irradiance

power through the cryopump baffle aperture (hits

the arm cavity baffle), W

Area of cryopump baf aperture, m^2

incident intensity, W/m^2

### Power Scattered into IFO Mode from Baffle Plate Edge

The scattered light from the ACB edge, as a function of tilt angle for edge radii 1, 2, and 4 mm, is shown in  Figure 12.

Figure 12: Power Scattered into the IFO Mode from the Baffle Plate Edge, Porcelainized Steel

### Power Scattered into IFO Mode from Baffle Plate Bend

The scattered light from the ACB bend as a function of tilt angle for edge radii 1, 2, and 4 mm is shown in Figure 13.

Figure 13: Power Scattered into the IFO Mode from the ACB Bend, Porcelainized Steel

Note that minimum scattering occurs when the baffle is tilted to approximately 1 deg, for this particular BRDF function.

### Total Power Scattered into IFO Mode from Baffle Plate Edge, Bend, and the Louver Surfaces of the ACB

The louver surfaces of the ACB are inclined at an incidence angle of 57 deg. The frontal area of the louver surfaces is

AACB = 0.236 m^2

The power into the IFO mode by the louver surface is given by

The BRDF of porcelainized steel at the incident angle of the louver plates is

The total scattered power by all parts of the ACB is given by

### Displacement Noise Due to Total ACB Scatter

#### Porcelainized Steel Scatter Noise

The displacement noise @ 100 Hz due to the ACB scatter, as a function of tilt angle, is shown in

ACB displacement @ 100 HZ, m/rt HZ

Figure 14: Displacement Noise, Total ACB Scatter, Porcelainized Steel

The glint portion of the displacement noise can be eliminated by tilting the ACB at 1 deg, so that the scattering from the louver surfaces dominates.

#### Oxidized Polished Stainless Steel Scatter Noise

The large angle BRDF of the oxidized stainless steel is approximately two times larger than that of porcelainized steel.

The displacement noise from scattering by the higher BRDF oxidized polished stainless steel is slightly larger than for the porcelainized steel, as shown in the Figure 15. For oxidized polished stainless steel, the scatter from the louver surface is larger than the glint from the edges and dominates the scatter at all tilt angles.

Figure 15: Displacement Noise, Total ACB Scatter, Porcelainized Steel and Oxidized Polished Stainless Steel

# Text boxes

θs

θxy

θs

θxy

2θi

2θi

θt

θi