| AUTHOR(S) | DATE | Document Change Notice, Release or Approval |
| --- | --- | --- |
| Jeff Lewis | 3/1/2011 | see LIGO DCC record Status |

# Scope

This document defines the requirements for music wire to be used in the Advanced LIGO suspension systems.

# Requirements

## General

- The wire shall be manufactured per ASTM A 228/A 228M, including, but not limited to, the chemical, mechanical, and metallurgical requirements.

- Diameter tolerance (inches): +/-0.0001 for wire ≤0.011 inches, +/-0.0002 for wire >0.011 and ≤0.02 inches, and +/-0.0005 for wire >0.02 and ≤0.032 inches.

- Minimum 12 inch cast at 12 inch length.

## Processing

- Clean gloves must be worn at all times.  (No bare hands touching the wire)

- Wire must be fresh drawn within 2 weeks of shipment

- Wire must be free of oil and grease and must not be used during the manufacturing process

## Inspection and Documentation

- Wire must be free of rust, scale, corrosion, spotting artifacts, die marks, pits, and scratches visible at 10X magnification

- Provide Material Certifications

- Provide Certificate of Conformance to Purchase Order requirements

## Packaging

- Wire shall be wound on 12 inch diameter spools

- Wire shall be tightly wrapped with anti-corrosion paper and taped

- Desiccant shall be added inside plastic shipping bag

- Purge plastic shipping bag with inert gas before sealing

- Double bag