## Slide 1: Growth and characterization of III-V epitaxial mirror coatings on silicon
Angie C. Lin1, Ashot S. Markosyan1, Riccardo Bassiri1, Alan Cumming2, Iain Martin2, Karen Haughian2, Roger Route1, Brian Lantz1, James S. Harris1, Sheila Rowan2, Martin M. Fejer1
1 Stanford University
2 University of Glasgow
Gravitational Wave Advanced Detector Workshop
May 14, 2012

## Slide 2: Single crystalline coatings
For third generation detectors operating at cryogenic temperatures:
Low mechanical loss in silicon at low T
Silicon is available in large sizes:
  Commercially available: 300 mm (12”)
  Research: 450 mm (18”)
Single crystalline coatings have already been shown to have low mechanical loss2
Loss sources in a Si flexure1
[1] Nawrodt et al. arXiv:1003.2893v1 (2010). [2] Cole et al. Appl. Phys. Lett. 92, 261108 (2010).
Notes: Silicon high Q, good bonding with epitaxial coating
Amorphous at low temp

## Slide 3: Direct integration of mirrors onto Si
Materials systems with index contrast but no change in lattice constant

## Slide 4: Integration approaches
Si substrate
AlP
GaP
Si substrate
AlAs
GaAs
SiGe buffer
Ge
AlAs
GaAs
Si substrate
Lift-off from GaAs substrate and bond to Si
Commercially available GaAs: 6”
Dislocations in SiGe arise from 4% mismatch between Si and Ge
Lattice-matched system, but less studied

## Slide 5: Outline
Epitaxial integration of III-V coatings on Si
Anticipated challenge: antiphase domains
  Growth technique: molecular beam epitaxy
  Film characterization techniques
  Reducing antiphase domains through growth conditions
GaP/AlP mirror coating on Si: initial results
  Materials characterization
  Optical absorption
  Mechanical loss
Summary and future work

## Slide 6: Anticipated challenge: antiphase defects
APB
GaP
Si
antiphase domain (APD)
Antiphase boundary (APB): defect with incorrect bonds (P-P or Ga-Ga)
Double atomic steps on Si surface
 correct bonds
Single atomic steps on Si surface
 wrong bonds
Notes: Si and GaP have the same crystal structure, except that there are two different atoms in GaP that make up the face-centered cubic sublattices. Because there’s no natural preference for Ga or P to settle into one sublattice versus the other, both will occur. When this happens, this defect is an antiphase boundary.

## Slide 7: Growth by molecular beam epitaxy
Sources and components:
Group III: Ga, Al, In
Group V: As, P
Group IV: Ge, Si
In-situ reflection high-energy electron diffraction (RHEED)
Advantages of using MBE:
Low impurity incorporation (UHV)
Monolayer control
Growth rate and substrate temperature decoupled
Control over growth rate, substrate temp, V/III flux ratio
substrate
sources
shutter
Notes: MBE is done under ultra-high vacuum where high-purity, elemental sources are evaporated onto a substrate. The sources are contained inside a crucible that is heated up to a temperature where the material starts to evaporate or sublimate and there is direct line-of-sight from the source to the substrate, where deposition occurs. Each source has a shutter in front of it to block the material from reaching the substrate when that material isn’t being deposited.

## Slide 8: Ex-situ characterization techniques
A film with many antiphase domains
100 nm
100 nm
Detect APDs with atomic force microscopy (AFM) and transmission electron microscopy (TEM)
AFM: surface pit density
TEM: how APBs propagate in the film
Sample courtesy of D. Liang, Y. Kang (Stanford)

## Slide 9: Achieving high quality GaP on Si
A.C. Lin et al. J. Vac. Sci. Technol. B 29 (2011) 1201.
Si
GaP
50 nm
GaP
Si
0
-3
3
nm
GaP overgrowth:
Annihilate defects
Si
1 μm
1 μm
0
0
Si surface prep:
Standard clean
Si buffer
High T anneal
0
-1
1
nm
Si
Si
2 nm
III-V
III-V nucleation:
2D growth
0
-2
2
nm
Notes: AFM shows film surface: start with a Si surface with rms roughness of about 0.1-0.2 nm.

## Slide 10: Outline
Epitaxial integration of III-V coatings on Si
Anticipated challenge: antiphase domains
  Growth technique: molecular beam epitaxy
  Film characterization techniques
  Reducing antiphase domains through growth conditions
GaP/AlP mirror coating on Si: preliminary results
  Materials characterization
  Optical absorption
  Mechanical loss
Summary and future work

## Slide 11: Epitaxial GaP/AlGaP layers on Si
Dispersion relations from N.A. Pikhtin et. al. Soviet Phys. 9 (1967) 107.
Transfer matrix Matlab code courtesy of Tomás Sarmiento (Stanford)
Theoretical reflectivity (%)
83%
At 1550 nm:
nGaP = 3.05
nAlGaP = 2.77
nSi = 3.42
Number of pairs
Si substrate (~525 μm)
200 nm GaP buffer
140 nm Al0.9Ga0.1P
127 nm GaP
Mirror pairs
Al0.9Ga0.1P
GaP
Index contrast Δn = 0.28
Pure AlP oxidizes easily

## Slide 12: Achieved expected reflectivity
Wavelength (nm)
Measured reflectivity (%)
Reflectivity (normalized)
Wavelength (nm)
measured
simulated
For 10 pairs: measured reflectivity matches theoretical reflectivity (83%)

## Slide 13: Transmission electron microscopy
1 μm
100 nm
100 nm
Bright-field 110 TEM: mass contrast
buffer
mirror pairs
100 nm

## Slide 14: Optical absorption
Using photothermal common-path interferometry (PCI) to measure absorption
Possible source of absorption: free carriers in GaP1,2
  Si outdiffusion from substrate
  Carbon, oxygen incorporation
  Antiphase domains (Ga-Ga, P-P)
Low temperature will freeze out the carriers
2.2 eV
[1] P.J. Dean et al. J. Appl. Phys. 39, 5631 (1968).
[2] K.W. Nauka, Imperfections in III/V Materials (1993).
Ec
Ev
C (EA = 48 meV)
Si (EA = 204 meV)
Si (ED = 80 meV)
PGa (ED = 230 meV)
Notes: A possible source of absorption is the presence of free carriers. This can come from impurities in the mirror layers, such as Si outdiffusion from the substrate or carbon and oxygen incorporation from substrate cleaning processes or growth itself. The antiphase domains may also act as acceptors and donors due to the fact that they are not charge neutral. While free carriers can be a problem at room temperature, they are expected to freeze out at low temperature and not contribute free carrier absorption. Low temperature absorption measurements are underway.

## Slide 15: Secondary ion mass spectroscopy
Si substrate
GaP buffer
AlGaP
GaP
Is there a source of free carriers?
C, O present at Si/GaP interface
Si diffusion limited to GaP buffer layer
SIMS done by Evans Analytical Group
Notes: C, O present at Si/GaP interface, likely due to transfer between the Si and GaP deposition steps. No significant Si diffusion- the concentration of Si drops from 5e22, the concentration in the Si substrate to below 1e16 or the background noise level within 50 nm. This is contained in the GaP buffer layer.

## Slide 16: Initial results for mechanical loss
8000
16000
12000
18000
20000
Frequency (Hz)
0
2×10-5
4×10-5
6×10-5
8×10-5
1×10-4
Measured loss
Uncoated Si disk
Coated Si disk
No discernible difference between lowest measured losses in coated and uncoated samples

## Slide 17: Summary and future work
GaP/AlP mirrors can be grown directly on Si
Challenges with epitaxial integration onto Si can be addressed by nucleation and growth conditions
Preliminary structural, optical absorption, and mechanical loss measurements have been done on GaP/AlGaP mirrors
Future work:
Low temperature absorption measurements
Low temperature mechanical loss measurements
Investigating other growth conditions to further reduce defects and impurities
Acknowledgements: This work was supported by NSF grant PHY-10 68596.

## Slide 19: Material properties
Material | Lattice constant (Å) | Mismatch (%) | Refractive index (near-IR) | Linear thermal expansion coefficient (°C-1)
AlP | 5.4510 |  | 2.75 | 6.10*10-6
GaP | 5.4505 | 0.4 | 3.02 | 4.65*10-6
Si | 5.4310 |  | 3.42 | 2.60*10-6
AlAs | 5.6611 |  | 2.86 | 5.20*10-6
GaAs | 5.6533 | 0.08 | 3.30 | 5.73*10-6
Ge | 5.6580 |  | 4.00 | 5.90*10-6
z

## Slide 20: In-situ characterization: RHEED
1-3°
Monoenergetic
electron gun
wafer
Phosphor screen
Sampling size ~ 1x5 mm
P
Ga
GaP (001) 2x4 surface
Beam along [110]
Beam along [110]
Observe how the film is growing: island or 2D growth mode
Smooth surface
Rough surface
S.A. Chambers, Surf. Sci. Rep. 39, 105 (2000).
Notes: RHEED is especially important for characterizing polar-on-nonpolar films because you can tell what the orientation of the film is. A streaky pattern is observed when the surface is reconstructed and atoms have periodic order. RHEED indicates 2-dimensional growth, whereas spots would indicated island growth. So during the deposition process, we already have an idea of the film quality. These are examples the streaky RHEED patterns we see when we deposit GaP on Si in a well-controlled manner.

## Slide 21: Achieving high-quality GaP on Si
In order of growth sequence:
Start with a smooth, double-stepped Si surface
  High temp anneal under H2 flow 1
Reduce APD formation
  2D nucleation of GaP on Si 2-5
Encourage APD annihilation
  Control APB propagation 6
1 B. Kunert et al. Thin Solid Films 517 (2008) 140. 4 I. Nemeth et al. J. Crys. Growth 310 (2008) 1595.
2 K. Yamane et al. J. Crys. Growth 311 (2009) 794. 5 A.C. Lin et al. J. Vac. Sci. Technol. B 29 (2011) 1201.
3 T.J. Grassman et al. Appl. Phys. Lett. 94 (2009) 232106. 6 X. Yu et al. J. Crys. Growth 301-302 (2007) 163.
Si
Si
Si
GaP

## Slide 22: Control GaP orientation with temperature
Sample | A | B | C | D
Nucleation layer | 525°C | 500°C | 325°C | 325°C
GaP film | 525°C | 550°C 600°C | 550°C | 550°C 600°C
RHEED | 4x2 | 4x2 | 2x4 | 2x4
orientation | - | - | + | +
High T nucleation
Low T nucleation
2x
4x
rms = 1.93 nm
rms = 1.74 nm
A
D
[110]
[110]
Notes: I previously mentioned that in MBE, we have 3 main parameters to work with: growth rate, V/III flux ratio, and substrate temperature. In fact, we use substrate temperature to select the orientation that we wish to grow. The table shows 4 different samples, all grown using a two-step process with a nucleation step and a subsequent growth step.

## Slide 23: Need well-controlled nucleation
K. Yamane et al. J. Crys. Growth 311 (2007) 794-797.
MEE
Ga
P
MBE
Ga
P
20 nm
GaP film nucleated with
migration enhanced epitaxy (MEE)
GaP
Si

## Slide 24: Two-dimensional III-V film on Si
nm
0
-2
2
0
500
nm
0
500
nm
1000
1000
rms = 0.961 nm
rms = 0.863 nm
rms = 0.279 nm
4 ML MEE GaP
Si
4 ML MEE GaP
2 ML MBE GaP
Si
4 ML MEE Al0.5Ga0.5P
2 ML MBE Al0.5Ga0.5P
Si
growth direction
A.C. Lin et al. J. Vac. Sci. Technol. B 29 (2011) 1201.
3x reduction in rms roughness with addition of Al

## Slide 25: Abrupt interface between III-V and Si
GaP MEE
GaP MBE
Si
3 nm
AlGaP MEE
AlGaP MBE
Si
2 nm
A.C. Lin et al. J. Vac. Sci. Technol. B 29 (2011) 1201.
glue
glue

## Slide 26: Effect of the first 5 monolayers
200 nm GaP
5 ML GaP
Si
200 nm GaP
5 ML Al0.5Ga0.5P
Si
rms = 0.50 nm
rms = 2.28 nm
A.C. Lin et al. J. Vac. Sci. Technol. B 29 (2011) 1201.
50 nm
GaP
Si

## Slide 27: Using TEM to view APDs
DF 200
50 nm
DF 200
50 nm
GaP
Si
APDs of opposite polarity have contrast under certain diffraction conditions  distinguish antiphase boundaries from other defects (stacking faults, dislocations)