## Slide 1: Coating-reduced interferometer optics
Resonant waveguide gratings
S. Kroker, T. Käsebier, E.-B. Kley, A. Tünnermann

## Slide 2: Coating-reduced interferometer optics Outline
Outline
RWGs as mirrors
Advanced grating concepts
Fabrication
Optical losses
Summary & Outlook
Notes: RWG mirrors … advanced grating concepts?

## Slide 3
Coating-reduced interferometer optics Introduction
Introduction – coating thermal noise
strain sensitivity
frequency
seismic /
radiation pressure
shot noise
coating thermal noise
Notes: „Brownian“ in Überschrift?

## Slide 4
Introduction – reducing coating thermal noise
conventional: dielectric amorphous multilayer stack
reflectivity
99.996% reflectivity
Brownian coating thermal noise
multiple beam interference:
Harry et al. , CQG (2002)
SiO2/Ta2O5
~3…8 µm
Coating-reduced interferometer optics Introduction
Possibility- optimization materials: crystalline coatings (AlxGaAs)
See talk by G. Cole!
crystalline

## Slide 5
Coating-reduced interferometer optics
Introduction - RWGs
<1 µm
high-index
low-index
Popov et al., Opt. Comm .(1985)
Brückner et al., PRL (2010)
Possibility- alternative optical concepts + material optimization:
Resonant waveguide gratings (RWGs)
Origin: weakly modulated high-index grating
on low-index substrate (narrow band)
Stronger modulation: larger bandwidth
Replace low-index substrate
Replace low-index material
no coating

## Slide 6: Coating-reduced interferometer optics RWG mirrors
Tantala grating on silica for 1064 nm
Monolithic silicon gratings for 1550 nm
Friedrich et al., Opt. Express (2011)
Brückner et al., Opt. Express (2008)
Brückner et al., PRL (2010)
reflectivity
measurements
in cavity
RWGs as mirrors – so far
Notes: Unterschied in den setups im wesentlichen nur, dass tantala als einkoppelspiegel, daniels rauschpaper noch zitieren

## Slide 7: Coating-reduced interferometer optics Characterization of RWGs
Stabilized
PDH-error signal
Reflected light
D.Friedrich et al. Opt. Express 19, 14955 (2011)
Finesse= 790 (±100) → R ≥ 99.2(±0.1)%
Cavity stabilization with standard PDH-technique
Tantala RWG
Notes: Technical feasability was shown

## Slide 8
nh
nl
transmission
n=1
Functionality of RWGS – horizontal modes
~ 100% reflectivity
silicon as high-index material
(nh=3.48 @ l=1550 nm)
0th diffraction order
outside grating
1st diffraction orders
in grating
-1
1
p… grating period
Coating-reduced interferometer optics
Functionality of RWGs
l/nh<p<l/nl
Notes: Raypicture oder perturbed waveguides

## Slide 9
Botten et al., Opt. Act. (1981)
periodic array of slab waveguide
2nd mode
grating
ridge
Functionality of RWGS – vertical (Bloch-) modes
fundamental
mode
1st mode
x
z
TM-Modes
incident
light
Coating-reduced interferometer optics
Functionality of RWGs

## Slide 10
Effective index dependent on:
fill factor
period/ wavelength
polarisation
angle of incidence
High efficiency:
2 propagating modes (neff2>0)
1 propagating mode
TM-polarization
2 modes in
upper layer
x
Coating-reduced interferometer optics
Functionality of RWGs
1 mode in
lower layer

## Slide 11
mechanism for R=100%:
phase difference due to different effective indizes (different kz),
reflection/ interference at boundaries
no additional phase in lower grating
Amplitudes of grating modes need to
cancel out
x
z
Lalanne , J. Lightwave Tech. (2006)
Karagodsky et al., Opt. Express (2009)
exact intensities and phases + physical insight
incident
light
Coating-reduced interferometer optics
Functionality of RWGs

## Slide 12
Feel free to join!
D. Friedrich
K. Yamamoto
S. Vyatchanin
S. Hild
… interaction of light with surface structure…
Coating-reduced interferometer optics
RWGs
D. Heinert
R. Nawrodt
S. Kroker
Notes: Homogene schichtgeschichte von daniel und kazuhiro erwähnen

## Slide 13
1 µm
platinum
240 nm
pre-structured wafer
depth
 | grating | LIGO
ROC (m) | 0.6 | ~2000
rMirror (m) | 0.0035 | 0.17
depth (µm) | ~10 | ~7
Coating-reduced interferometer optics
Advanced grating concepts -Focusing Mirrors
maximum reflectivity : 97% ( l=1396 nm, q=5°)
resonance to larger wavelength with larger period/thickness...
Mirrors on Curved Substrates
Notes: ET: ~8 µm

## Slide 14
grating 1
grating 2
Thickness determines wavelength/ angle of max. reflection
entire
system?
1. stacked RWGs
enhance angular/ spectral bandwidths
enhance experimentally feasible reflectivity
Coating-reduced interferometer optics
Advanced grating concepts – stacked RWGS
Notes: Brauch noch ein Spektrum

## Slide 15
2. RWGs with 2D periodicity
Coating-reduced interferometer optics
Advanced Grating Concepts - 2D RWGs
basis for flat focusing mirrors
1 µm
2d a-Si grating

## Slide 16
Combination von highly efficient mirrors with diffraction grating
high Finesse
only weak perturbation
only 0th order
Highly efficient mirror
Diffraction grating
0th, ±1st orders
transversal
modulation:
Grating depth
lateral
Modulation:
Ridge width/
-position
Coating-reduced interferometer optics
Diffractive elements
High angular tolerance of reflector necessary
pmirror<l
pdiff=l... 2l

## Slide 17
electron-
beamresist
silicon
SiO2
electronbeam-
lithography +
development
anisotropic etching
process+
sidewall
passivation
isotropic
etching process
Fabrication
chromium
More complex
structures?
5 µm
Coating-reduced interferometer optics
Fabrication
2 µm

## Slide 18
R=(99.8±0.01)%
material properties
structure
deviations
systematic
(ridgewidth/-depth)
transmission
stochastic
(line edge roughness)
scattered
light
absorption
2 µm
Coating-reduced interferometer optics
Optical losses
Where is the missing light?
See talk by J. Komma!
Notes: Strukturen… Kantenrauhheit… Resist.. lack

## Slide 19
HSQ (1300 µC/cm2)
high sensitivity
(60 e-/100 nm2)
100 nm ridges and grooves
Line edge roughness due to particle statistics in the lithographic process
10nm
10nm
electron impacts
low sensitivity
(8000 e-/100 nm2)
FEP 171 (9.5 µC/cm2)
M. Heusingen, diploma thesis (2011)
Coating-reduced interferometer optics
Optical losses
Notes: Problem existiert – geringe Empfindlichkeit hohe Empfindlichkeiten, sehr aufw. Rigor. Rechnungen, einfluss auf Streulicht nachgewiesen -> neue Lösungen her – Bezug zu den anderen 2 Gebieten –

## Slide 20
Grating accuracy
+ 6.3 nm
- 6.6 nm
19 mm
50mm
position [mm]
period variation (pm)
period variation < 5 pm
wave-front measurement (1 µm period grating + technology, Littrow-Mount, l=633 nm)
significantly better than interferometric gratings
Coating-reduced interferometer optics
Optical losses
 | wavefront | placement
PV | 12.8 nm | < 10.3 nm
rms | 1.4 nm | < 1.1 nm
Notes: Experiment set up…. To measure scattered light @ 1550 nm

## Slide 21
Sophisticated device for measurement of scattered light ALBATROSS
at Fraunhofer Institute IOF
Measurements of scattered light at 1550 nm set up right now!
Coating-reduced interferometer optics
Optical losses

## Slide 22
Summary
Coating-reduced interferometer optics
Summary
RWGs capable of providing high reflectivity
Experiments for higher R running
Origin of optical losses to be identified
Thermal noise to be investigated