## Slide 1: Adventures in AR Absorption with aLIGO Core Optics
LSC-VIRGO , 2012
Margot Phelps
GariLynn Billingsley
Liyuan Zhang
Optical Coatings

## Slide 2: Outline
AR and HR
Tantala thin films
Compensation Plate Coating loss
Anneal Temperature
AR coatings- aLIGO Beamsplitter
AR coatings- aLIGO Compensation Plate
Trial and error!
Real mechanisms behind AR absorption
Notes: Purpose of talk! Theorical vs engineering channel Feynman, conversational dinner, exciting!!

## Slide 3: HR and AR Coatings on Recycling Cavity Optics
aLIGO COC optical coatings- made up of silica (SiO2) and tantala (Ta205) layers of varying width.
Coating absorption- Strict absorption requirements for all aLIGO coatings on optics, <1ppm
Harder to meet this on AR than on HR
  Can achieve <1ppm for HR, AR is much more sensitive.
HR coatings-not worried about transmission
  Tantala is used deeper in the stack, and in thicker layer
AR coatings- power transmission throughout all layers, not just the top as in HR.
Notes: Basic view of optical coatings. Want HR caotings to be highly reflective and ar coatings not to reflect. Simple enough.
But we want them to do this as perfectly as possible. Coatings cannot absorb, scatter, or reflect/transmit more than they should.

## Slide 4: Why use thin film tantala?
Stress Balance
  beam splitter design
Aspect ratio
  Test masses: ~2:1
  Beamsplitters ~6:1
Power term measured before coating BS02: 4.66nm
Measured after coating BS02: 5.8nm (G. Billingsley)
But the downsides..
Mismatched IBS coating stress
HR
AR
HR > AR
Notes: Power term means sag…elaborate

## Slide 5: 4 Examples-HR side of each

## Slide 6: Same optics-AR side

## Slide 7: Comparison of Beamsplitter HR Absorption(measured at Caltech)
Optic serial number | -x(avg) | +x(avg) | -y(avg) | +y(avg)
BS03 | 0.48ppm | 0.45ppm | 0.5ppm | 0.37ppm
BS05 | 0.29ppm | 0.29ppm | 0.29ppm | 0.29ppm
BS06 | 0.29ppm | 0.29ppm | 0.29ppm | 0.29ppm
Arrow
+y
+x
-x
-y
Measured a 20mm line
on each axis

## Slide 8: Comparison of Beamsplitter AR Absorption(measured at Caltech)
Optic serial number | -x(avg) | +x(avg) | -y(avg) | +y(avg)
BS03 | 4ppm | 2.7ppm | 11ppm | 2ppm
BS05 | 16ppm | 16ppm | 50ppm | 4ppm
BS06 | 1.6ppm | 1.8ppm | 0.9ppm | 1.4ppm
Arrow
+y
+x
-x
-y
Optic serial number | -x(avg) | +x(avg) | -y(avg) | +y(avg)
BS03 | 4ppm | 2.7ppm | 11ppm | 2ppm
BS05 | 16ppm | 16ppm | 50ppm | 4ppm
BS06 | 1.6ppm | 1.8ppm | 0.9ppm | 1.4ppm
Measured a 20mm line
on each axis

## Slide 9: Is it impossible to get a low loss AR? Actually, no.
We have optimized our CP design through trial and error

## Slide 10: Differences in BS and CP coating Designs
CP BS
Coating
Substrate
SiO2
Ta205
Ta205
SiO2
SiO2
Ta205
Air

## Slide 11: CPs: Exploring AR Absorption layer by layer
Notes: Thickness calculation based on the spectrum measured after each etch

## Slide 12: Goldilocks and the AR Absorption 300 C°, Too cold
Anneal and absorption measurements done at CIT: Phelps and Zhang
Advanced LIGO
No initial anneal
Notes: As is = no post deposition anneal
Design < 1/20 wave Tantala + ¼ wave Silica

## Slide 13: AR Absorption 350 C° Still too cold
Anneal and absorption measurements done at CIT: Phelps and Zhang
Advanced LIGO
No initial anneal
Notes: As-Is = No post deposition anneal

## Slide 14: AR Absorption 375 C° getting warmer
Anneal and absorption measurements done at CIT: Phelps and Zhang
Advanced LIGO
350 C initial anneal
Notes: 350C post deposition

## Slide 15: AR Absorption 425 C° too hot
Anneal and absorption measurements done at CIT: Phelps and Zhang
Advanced LIGO
350 C initial anneal

## Slide 16: AR Absorption 400 C° Just right!
Anneal and absorption measurements done at CIT: Phelps and Zhang
Advanced LIGO
350 C initial anneal
Notes: 350 C. post depsition anneal

## Slide 17: Conclusion
Found clues to mechanisms behind AR absorption
  Absorption is either in the tantala layers or in the interfacial layer between the tantala and silica(from etching tests)
  Anneal environment is important, esp. temperature(from anneal tests)
  Tantala film thickness and position in coating stack(looking at CP vs BS)
  HR behaves differently than AR(no energy in deeper layers of HR)
the CP design has been optimized, now applying those lessons to correct the beamsplitter absorption
Hope to help answer some fundamental questions about how tantala coatings work