| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: L. BARSOTTI | 02-20-13 |  |  |  |  |  |  |
| CHECKED: |  |  |  |  |  |  |  |
| APPROVED: P.FRITSCHEL |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

# Description

Plano/Curved reflectors for HAM6 telescopes when operating the IFO in low power mode

# Material

Corning HPFS 7980 (high purity fused silica, UV grade)

Grade 0G (or better)

# Dimensions

Diameter: 2” +0.000/-.005”

Thickness (center): 0.375” ± 0.005”

# Radius of Curvature (ROC):

Side 1: ROC R1 = + 4.6m ± 0.09m

Side 2: Flat

Fig2: Schematic picture of the curved optic. This picture has the only purpose of identifying the ROC of the optic and the two sides.

# Surface Roughness

Side 1

Super-polished less than 1 Angstrom over central 80% of diameter with 10-5

scratch-dig; best effort for 0/0 20-10 scratch-dig outside central 80% of diameter.

Side 2

Commercial-polish

Less than 5 Angstrom over central 80% of diameter

Edges and Bevels

Commercial-polish

# Surface Figure

Side 1

Flat < λ/10 at 632.8 over central 80%

Side 2

Flat < λ/4 at 632.8 over central 80%

# Coating

Wavelength: 1064nm

Angle of incidence: 0° -15°, p-pol

Side 1

T = 5% + 0.5% (not less than 5%)

Side 2

AR coating, R < 0.1% (best effort)

# Serial numbers:

Each optic will be serialized as follows:

E1201104 ROC = +4.6m, T=5%, S/N: 1 (2,3,4,5)

Serial numbers and registration marks shall be scribed or etched on the barrel of	the optic for in-vacuum use.

# Vendor to provide:

  - 1. Three spectrophotometer graphs of the reflectance and transmittance of the HR coatings; one covering the spectrum from 500nm to 1200nm; the others, with increased sensitivity, showing wavelengths from 900nm to 1100nm and from 500nm to 600nm

            - 2. Spectrophotometer graphs of the reflectance of the AR coating taken as cited above.

            - 3. Measurement of the ROC of the substrate