ASER INTERFEROMETER GRAVITATIONAL WAVE OBSERVATORY

LIGO

CALIFORNIA INSTITUTE OF TECHNOLOGY

MASSACHUSETTS INSTITUTE OF TECHNOLOGY

LIGO- T1300731 -v1 13 September 2013

Low-Scatter Coating for Stainless Steel Baffles

Michael Smith

LIGO Hanford Observatory			LIGO Livingston Observatory

P.O. Box 1970; Mail Stop S9-02		19100 LIGO Lane

Richland, WA 99352			Livingston, LA 70754

Phone (509) 37208106			Phone (225) 686-3100

Fax (509) 372-8137				Fax (225) 686-7189

E-mail: info@ligo.caltech.edu		E-mail: info@ligo.caltech.edu

California Institute of Technology		Massachusetts Institute of Technology

LIGO – MS 100-36				LIGO – MS NW22-295

Pasadena, CA 91125				Cambridge, MA 02139

Phone (626) 395-2129				Phone (617) 253-4824

Fax (626) 304-9834				Fax (617) 253-7014

E-mail: info@ligo.caltech.edu		E-mail: info@ligo.mit.edu

CHANGE LOG

| Date, version | Summary of Changes |
| --- | --- |
| 8/27/13 V1 | New document |

Table of Contents

1	Introduction	6

1.1	ACB Scattering Surfaces	7

2	Scattering Analysis	12

2.1	Scattering Parameters	12

2.2	Oxidized Stainless Steel Baffle	15

2.2.1	Scatter from Photodetectors	15

2.2.2	Scatter from Screw Heads	16

2.2.3	BRDF of Oxidized Stainless Steel	17

2.2.4	Scatter by Oxidized SS Baffle Hole Edge	18

2.2.5	Scatter by Oxidized SS Baffle Center Plate Edge	19

2.2.6	Scatter by Oxidized SS Baffle Bend	19

2.2.7	Scatter by Oxidized SS Louver Baffle Portion	20

2.2.8	Total Scatter by Oxidized SS ACB	21

2.3	Multilayer AR Coating on Stainless Steel	22

2.3.1	BRDF and Reflectivity of Multilayer AR Coating	22

2.3.2	Scatter by Multilayer AR Coating on SS Baffle Hole Edge	24

2.3.3	Scatter by Multilayer AR Coating on SS Center Plate Edge	25

2.3.4	Scatter by Multilayer AR Coating on SS Louver Bend	25

2.3.5	Scatter by Multilayer AR Coating on SS Louver Baffle Portion	26

2.3.6	Scatter from Screw Heads	27

2.3.7	Scatter from Photodetectors	27

2.3.8	Total Scatter by Multilayer AR Coating on SS ACB	27

2.4	DLC Coating on Stainless Steel	30

2.4.1	BRDF and Reflectivity of DLC Coating	30

2.4.2	Scatter by DLC Coating on SS Baffle Hole Edge	33

2.4.3	Scatter by DLC Coating on SS Center Plate Edge	34

2.4.4	Scatter by DLC Coating on SS Baffle Bend	35

2.4.5	Scatter by DLC Coating on SS Louver Baffle Portion	35

2.4.6	Scatter from Screw Heads	36

2.4.7	Scatter from Photodetectors	36

2.4.8	Total Scatter by DLC Coating on SS ACB	36

3	Conclusions	38

3.1	Comparison of Scattered Light Displacement Noise, m/rtHz from Multilayer AR Coating ACB and DLC Coating ACB with Default aLIGO Oxidized SS ACB	38

3.2	Limiting Scattering Sources	38

3.2.1	Edge Scatter	38

3.2.2	Screw Head Scatter	38

3.3	BRDF	38

3.4	Reflectivity	38

4	Reference Data	39

Table of Figures

Figure 1: Arm Cavity Baffle Showing Principal Scattering Surfaces	7

Figure 2: Frontal Area of ACB Hit by Narrow Angle Scatter from Far Test Mass Mirror	8

Figure 3: Cross-section of ACB	8

Figure 4: Bend Radius of ACB Used in the Scattered Light Calculation	9

Figure 5: Edge Radius of Central Plate Used in the Scattered Light Calculation	10

Figure 6: Actual Cross Section of ACB SS Hole Beveled Edge	11

Figure 7: Measured BRDF Data, Oxidized Stainless Steel, with Parametric Fit	17

Figure 8: Parametric BRDF Functions, as Best Fit to CASI Data	18

Figure 9: Total Scattered Power, W, by Oxidized SS ACB vs Plate Edge Radius, m	21

Figure 10: Measured BRDF Data, Multilayer AR Coating on SS, with Parametric Fit	22

Figure 11: Parametric Functions for Multilayer AR Coating BRDF as Best Fit to CASI Data	23

Figure 12: Multilayer AR Coating Backscatter BRDF sr^-1 vs Incidence Angle, Deg	23

Figure 13: Reflectivity of Multilayer AR Coating vs Incidence Angle	24

Figure 14: Total Scattered Power, W, by Multilayer AR Coating on SS ACB vs Screw Head BRDF, sr^-1	27

Figure 15: Total Scattered Power, W, by Multilayer AR Coating on SS ACB vs Tilt Angle, Deg	28

Figure 16: Total Scattered Power, W, by Multilayer AR Coating on SS ACB vs Center Plate Edge Radius, m	28

Figure 17: Measured BRDF Data, DLC Coating on SS, with Parametric Fit	30

Figure 18: Parametric DLC Coating BRDF Functions, as Best Fit to CASI Data	31

Figure 19: Backscatter BRDF, sr^-1, DLC Coating as a Function of Incidence Angle, Deg	32

Figure 20: Reflectivity DLC Coating as a Function of Incidence Angle, Deg	33

Figure 21: Total Scattered Power, W, by DLC Coating on SS ACB vs Tilt Angle, Deg	36

Figure 22: Total Scattered Power, W, by DLC Coating on SS ACB vs Center Plate Edge Radius, m	37

# Introduction

An improved low-scattering and low-reflectivity coating for polished stainless steel was developed using a multilayer dielectric antireflection coating; the coating was applied by a commercial coating vendor using an ion assisted physical vapor deposition (PVD) process, in which an electron beam was used to evaporate the coating materials.

The BRDF and reflectance properties of the sample film were measured. The back-scatter BRDF at 57 deg incidence angle of the multilayer AR coating on SS is <1E-5 sr^-1 for p-polarization. The reflectivity of the multilayer AR coating on SS for 57 deg incidence angle is <1E-3 for both polarizations--i.e. > 99.9% of the incident power striking the louver portion of the ACB will be absorbed. This would be a very efficient baffle surface.

As an example of the use of this coating, the calculated scattered light noise from the aLIGO stainless steel Arm Cavity Baffle (ACB) with this multi-layer dielectric antireflection coating (mAR) is compared with a diamond-like coating (DLC), and with the aLIGO default oxidized stainless steel. An 80 times reduction in scattered light displacement noise could be obtained with the multilayer AR coating over the default oxidized SS ACB;  whereas, a 19 times reduction in scattered light displacement noise could be achieved with the DLC coating.

One caveat of the use of the multi-layer dielectric antireflection coating is that it probably will be restricted to a planar surface; whereas, the DLC coating can be applied to an arbitrarily shaped surface.

## ACB Scattering Surfaces

Figure 1: Arm Cavity Baffle Showing Principal Scattering Surfaces

Figure 2: Frontal Area of ACB Hit by Narrow Angle Scatter from Far Test Mass Mirror

Figure 3: Cross-section of ACB

Figure 4: Bend Radius of ACB Used in the Scattered Light Calculation

Figure 5: Edge Radius of Central Plate Used in the Scattered Light Calculation

Figure 6: Actual Cross Section of ACB SS Hole Beveled Edge

# Scattering Analysis

The scattered light from the surface of the far test mass mirror will pass down the interferometer arm, through the Manifold/Cryopump Baffle, and hit the Arm Cavity Baffle (ACB) in front of the near test mass.

## Scattering Parameters

Arm Power, W

radius of SS baffle edge, m

radius of SS baffle bend, m

length of baffle plate edge, m

length of baffle bend, m

Frontal area of SS center plate cut edge, m^2

Frontal area of SS baffle bend edge, m^2

BRDF of SS cut edge, sr^-1

BRDF of photodetector, sr^-1

BRDF of screw head sr^-1

number of photodetector

number of screw heads

radius of photodetector ring, m

Photoconductor radius, m

photoconductor area, m^2

Screw head radius (#10), m

Screw head area, m^2

laser wavelength, m

wave number, m^-1

ACB displacement @ 100 HZ, m/rt HZ

IFO waist size, m

solid angle of IFO mode, sr

Transfer function @ 100 Hz, ITM HR

IFO arm length, m

PSL laser power, W

Arm Power, W

radius of Cryopump aperture, m

half-angle from centerline to Rcp, rad

half-angle from centerline to Rcp, rad (see ACB_PD_scatter_8-29-12)

BRDF, sr^-1; CSIRO, surface 2, S/N 2

radius of manifold/cryo baffle, m

height of ledge, m

radius of ACB hole, m

area of ACB hole, m^2

thickness of baffle plate, m

maximum width of exposed edge, m

exposed area of baffle plate hole edge, m^2

area of manifold/cryo baffle ledge, m^2

area of exposed ACB, m^2

The intensity of the light incident on the ACB surface is calculated.

power through the cryopump baffle aperture

(hits the arm cavity baffle), W

Area of cryopump baf aperture, m^2

incident intensity, W/m^2

## Oxidized Stainless Steel Baffle

### Scatter from Photodetectors

Scatter from photodetectors

number of photodetector

photoconductor area, m^2

COC Scattered power hitting the PD, W

power scattered by photodetector,

into IFO mode, W

displacement noise @ 100 Hz, m/rtHz

### Scatter from Screw Heads

Scatter from screw heads

number of screw heads

Screw head area, m^2

COC Scattered power hitting

the screw head W

power scattered by screw head

into IFO mode, W

displacement noise @ 100 Hz, m/rtHz

### BRDF of Oxidized Stainless Steel

The incident angle of the light hitting the louver portion of the ACB is 57 deg, and the incident angle hitting the edge of the central plate and the hole of the baffle is centered at approximately 0 deg.

The BRDF, sr^-1 of oxidized polished stainless steel was measured with a CASI scatterometer at incidence angles of 57 deg and 3 deg as a function of the angle away from the specular direction.

Figure 7: Measured BRDF Data, Oxidized Stainless Steel, with Parametric Fit

The parametric curves shown below were fit to the CASI BRDF data.

The 3 deg data will be used for computing the normal incidence BRDF values. The BRDF data is approximately symmetrical for plus and minus angles about the specular direction.

Figure 8: Parametric BRDF Functions, as Best Fit to CASI Data

### Scatter by Oxidized SS Baffle Hole Edge

BRDF geometric scatter function from baffle hole edge

Scattered power into IFO from baffle hole edge

displacement noise @ 100 Hz, m/rtHz

### Scatter by Oxidized SS Baffle Center Plate Edge

Scatter from SS center plate edge

power incident on SS center plate edge, W

Scattered power into IFO from oxy SS center plate edge

displacement noise @ 100 Hz, m/rtHz

### Scatter by Oxidized SS Baffle Bend

BRDF geometric scatter function from oxy baffle bend

Scattered power into IFO from oxy SS baffle bend

displacement noise @ 100 Hz, m/rtHz

### Scatter by Oxidized SS Louver Baffle Portion

displacement noise @ 100 Hz, m/rtHz

### Total Scatter by Oxidized SS ACB

Figure 9: Total Scattered Power, W, by Oxidized SS ACB vs Plate Edge Radius, m

Note: the SS edge scatter does not dominate for edge radius < 0.003 m

total displacement noise @ 100 Hz, m/rtHz

## Multilayer AR Coating on Stainless Steel

### BRDF and Reflectivity of Multilayer AR Coating

The incident angle of the light hitting the louver portion of the ACB is 57 deg, and the incident angle hitting the edge of the central plate and the hole of the baffle is centered at approximately 0 deg.

The BRDF was measured for multilayer AR coating on SS at incidence angles of 57 deg, 30 deg, 15 deg, 10 deg, and 3 deg, as a function of the angle away from the specular direction. The 57 deg data with the parametric fit is shown below.

Figure 10: Measured BRDF Data, Multilayer AR Coating on SS, with Parametric Fit

The parametric curves shown below were fit to the CASI BRDF data.

The 3 deg data will be used for computing the normal incidence BRDF values. The BRDF data is approximately symmetrical for plus and minus angles about the specular direction.

Figure 11: Parametric Functions for Multilayer AR Coating BRDF as Best Fit to CASI Data

Back-scatter BRDF, sr^-1, as a function of incidence angle, deg, is presented below.

Figure 12: Multilayer AR Coating Backscatter BRDF sr^-1 vs Incidence Angle, Deg

Summary of reflectivity as a function of incidence angle is presented below.

Figure 13: Reflectivity of Multilayer AR Coating vs Incidence Angle

### Scatter by Multilayer AR Coating on SS Baffle Hole Edge

Scatter from oxy SS baffle hole edge

BRDF geometric scatter function from baffle hole edge

Scattered power into IFO from baffle hole edge

displacement noise @ 100 Hz, m/rtHz

### Scatter by Multilayer AR Coating on SS Center Plate Edge

Scatter from mAR-SS center plate edge

BRDF geometric scatter function from mAR-SS center plate edge

Scattered power into IFO from mAR-SS baffle center plate edge

displacement noise @ 100 Hz, m/rtHz

### Scatter by Multilayer AR Coating on SS Louver Bend

BRDF geometric scatter function from mAR-SS baffle bend

Scattered power into IFO from mAR-SS baffle bend

displacement noise @ 100 Hz, m/rtHz

### Scatter by Multilayer AR Coating on SS Louver Baffle Portion

Power Scattered from the mAR-SS louver portion of baffle

displacement noise @ 100 Hz, m/rtHz

### Scatter from Screw Heads

See section 2.2.1

### Scatter from Photodetectors

See section 2.2.2

### Total Scatter by Multilayer AR Coating on SS ACB

Reduce screw head BRDF by polishing so that louver dominates the scatter

Figure 14: Total Scattered Power, W, by Multilayer AR Coating on SS ACB vs Screw Head BRDF, sr^-1

Note: the screw head BRDF must be <  sr^-1 for louver scatter to dominate

Tilt the baffle so that edge scatter does not dominate

Figure 15: Total Scattered Power, W, by Multilayer AR Coating on SS ACB vs Tilt Angle, Deg

Note: the edge scatter does not dominate for tilt angles >0.3 deg

Figure 16: Total Scattered Power, W, by Multilayer AR Coating on SS ACB vs Center Plate Edge Radius, m

Note: the DLC edge scatter does not dominate for edge radius < 0.01 m

total displacement noise @ 100 Hz, m/rtHz

## DLC Coating on Stainless Steel

### BRDF and Reflectivity of DLC Coating

The incident angle of the light hitting the louver portion of the ACB is 57 deg, and the incident angle hitting the edge of the central plate and the hole of the baffle is centered at approximately 0 deg.

A DLC AR coating on SS was obtained from R. Takahashi of the KAGRA group. The

properties of this coating were previously reported by R. Takahashi et al. The film was deposited using direct current plasma chemical vapor deposition (CVD), 120 mA @ 500V.

The BRDF was measured for DLC coating on SS at incidence angles of 57 deg and 3 deg as a function of the angle away from the specular directions.

Figure 17: Measured BRDF Data, DLC Coating on SS, with Parametric Fit

The parametric curves shown below were fit to the CASI BRDF data.

The 5 deg data will be used for computing the normal incidence BRDF values. The BRDF data is approximately symmetrical for plus and minus angles about the specular direction.

Figure 18: Parametric DLC Coating BRDF Functions, as Best Fit to CASI Data

Back-scatter BRDF, sr^-1, as a function of incidence angle is presented below.

Figure 19: Backscatter BRDF, sr^-1, DLC Coating as a Function of Incidence Angle, Deg

Summary of reflectivity as a function of incidence angle is presented below.

Figure 20: Reflectivity DLC Coating as a Function of Incidence Angle, Deg

### Scatter by DLC Coating on SS Baffle Hole Edge

Scatter from DLC SS baffle hole edge

BRDF geometric scatter function from baffle hole edge

Scattered power into IFO from baffle hole edge

displacement noise @ 100 Hz, m/rtHz

### Scatter by DLC Coating on SS Center Plate Edge

Scatter from DLC-SS center plate edge

BRDF geometric scatter function from DLC-SS center plate edge

Scattered power into IFO from DLC-SS baffle center plate edge

displacement noise @ 100 Hz, m/rtHz

### Scatter by DLC Coating on SS Baffle Bend

Scatter from DLC-SS baffle bend

BRDF geometric scatter function from DLC-SS baffle bend

Scattered power into IFO from DLC-SS baffle bend

displacement noise @ 100 Hz, m/rtHz

### Scatter by DLC Coating on SS Louver Baffle Portion

Power Scattered from the DLC-SS louver portion of baffle

displacement noise @ 100 Hz, m/rtHz

### Scatter from Screw Heads

See section 2.2.2

### Scatter from Photodetectors

See section 2.2.1.

### Total Scatter by DLC Coating on SS ACB

Tilt the baffle so that edge scatter does not dominate

Figure 21: Total Scattered Power, W, by DLC Coating on SS ACB vs Tilt Angle, Deg

Note: the edge scatter does not dominate for tilt angles >1 deg

Figure 22: Total Scattered Power, W, by DLC Coating on SS ACB vs Center Plate Edge Radius, m

Note: the DLC edge scatter does not dominate for edge radius < 0.01 m

total displacement noise @ 100 Hz, m/rtHz

# Conclusions

## Comparison of Scattered Light Displacement Noise, m/rtHz from Multilayer AR Coating ACB and DLC Coating ACB with Default aLIGO Oxidized SS ACB

Comparison of mAR coated SS to oxidized SS baffle

Comparison of DLC coated SS to oxidized SS baffle

Based on measured BRDF data, a 19 times reduction in scattered light displacement noise could be achieved with the DLC coating, and an 80 times reduction in scattered light displacement noise could be obtained with the multilayer AR coating, in comparison with the default oxidized SS ACB.

## Limiting Scattering Sources

### Edge Scatter

The limiting scatter from the frontal edges of the baffle is effectively eliminated by tilting the baffle > 1 deg in the pitch direction.

### Screw Head Scatter

Scatter from the three screw heads around the periphery of each photodetector is a limiting scattering source for the case of the multilayer AR coated SS. This limiting scattering source can be eliminated by polishing the surfaces of the flat screw heads to achieve a BRDF <0.003 sr^-1.

## BRDF

The back-scatter BRDF at 57 deg incidence angle of the multilayer AR coating on SS is <1E-5 sr^-1 for p-polarization.

## Reflectivity

The reflectivity at 57 deg incidence angle of the multilayer AR coating on SS is <1E-3 for both polarizations.

# Reference Data

T1300716-v1_ACB Multi-AR coating on SS

T1300717-v1_BRDF Multi-AR SS 3 deg inc

T1300718-v1_BRDF Multi-AR SS 15 deg inc

T1300719-v1_BRDF Multi-AR SS 57 deg inc

T1300765-v1_BRDF Multi-AR SS 30 deg inc

T1300766-v1_BRDF Multi-AR SS 10 deg inc

T1300768-v1_DLC 5 deg inc

T1300767-v1_DLC 15 deg inc

T1300764-v1_DLC 57 deg inc

# Text boxes

Baffle Plate Hole Edge

Baffle Louver Bend

Center Plate

Edge

Cryo Baffle Opening

Photoconductor with 3 screw heads

Central plate edge radius

Radius = 0.1 mm

Baffle Louver