## Slide 1: Modeling Internal Friction in Amorphous Oxides Using Two-Level Systems
Chris Billman
9/18/2015

## Slide 2
http://10m-prototype.aei.uni-hannover.de/design-and-sensitivity
http://www.ligo.org/science/GW-Sources.php
I W Martin, Class. Quantum Grav. 2014.

## Slide 3: Outline
Describe Theory (W. A. Phillips Rep. Prog. Phys. 1987)
  Introduce two-level systems (TLS)
  Find the susceptibility
  Calculate the internal friction
Describe Model: Classical molecular dynamics (MD)
Apply the model to Ta2O5 and SiO2
Conclusion

## Slide 4: Two-Level System: The Basics
Rashid Hamdan, J. Phys. Chem 2014.

## Slide 5: Two-Level System: The Basics

## Slide 6: Two-Level System: Electric Susceptibility and Dipolar Relaxation

## Slide 7: Two-Level System: Mechanical Loss

## Slide 8: Classical MD Basics
Classical description of forces:
  Built on F=ma
  Interatomic potentials are modeled to fit experimental data (Density, elastic moduli, radial distribution functions, etc.)
  Potentials were developed by Jonathan Trinastic.
https://en.wikipedia.org/wiki/Buckingham_potential

## Slide 9: The TLS model in MD
Rashid Hamdan, unpublished.

## Slide 10: Model Inputs: TLS Distribution

## Slide 11: Mechanical Loss: Approximations
Asymmetry Cut-off
  Previously, a 0.1 eV asymmetry cut-off was used to better match experiment.
Ta2O5

## Slide 12: What our model contributes
Rashid Hamdan, J. Phys. Chem 2014.

## Slide 13: Conclusion
The acoustic loss in amorphous solids is a consequence of applying a mechanical field to systems of dipoles, and can be derived from a model Hamiltonian where we assume two-level systems where symmetry is broken by an applied field.
Using classical molecular dynamics to provide inputs for the TLS model gives good agreement with the low temperature peak. Using the 2-D distribution, more detailed features can be seen at higher temperature.
  For SiO2 this shows a second peak at 150K which matches experiment.
  For Ta2O5, it does not lead to a better description but better statistics may be required.
This allows us to
  Understand the atomic transitions that cause internal friction
  Predict internal friction under different doping
  Determine what causes higher temperature peaks

## Slide 14: Model Inputs: Elastic Moduli and Coupling

## Slide 15: Model Inputs: Relaxation Time