## Slide 1: Overview of coating thermal noise
Gabriele Vajente
LIGO Laboratory Caltech
GWADW 18
15th May 2018, Girdwood, Alaska
Image credits: LIGO/Joe Hanson
LIGO-G1800920-v4

## Slide 2: Advanced Detector Sensitivities
New aLIGO design curve from LIGO-T1800044-v5
Thermal noise measurement
Gras et al. arxiv:1802.05372
AdVirgo design curve
From Acernese et al. CQG 32, 024001 (2015)

## Slide 3: Coating Thermal Noise: a primer
Thermal (Brownian) noise:
  system in thermal equilibrium, couples energy to thermal bath through mechanical dissipations
  The reverse is true: energy coupled to the system (kBT per each mode), random over all frequencies
  The higher the dissipations, the more energy is spread out of resonance
Other sources of thermal noise: thermo-elastic, thermo-refractive
Power spectral density of fluctuations in the (mechanical) variable x
Imaginary part of the system transfer function (linked to dissipations)
Fluctuation dissipation theorem
H. B. Callen, T. A. Welton (1951). "Irreversibility and Generalized Noise". Physical Review. 83: 34

## Slide 4: How we make high reflection coatings
Alternate layers of high and low refractive index materials
Silica
Tantala*
Silica
Tantala*
Silica
Tantala*
Substrate
* Titania doped
Material | Refractive index | Loss angle (100 Hz)
Silica SiO2 | 1.45 | 0.5 x 10-4
Tantala Ta2O5 | 2.03 | 3.4 x 10-4
Titania-doped tantala Ta2O5-TiO2 | 2.07 | (original design*) 2.4 x 10-4 (MIT direct CTN*) 3.6 x 10-4
Interference of Fresnel reflections
The effective loss angle is a combination of those of the two materials: dominated by the high index material
*Class. Quantum Grav. 24 (2007) 405–415
**Phys. Rev. D 95, 022001

## Slide 5: The future
Exploring the sensitivity of next generation gravitational wave detectors
CQG 34, 044001 (2017)
M. Evans G1800462

## Slide 6: Future coatings: different requirements
 | aLIGO | aLIGO+ | AdVirgo+ | Voyager | C.E. | E.T.
Temperature | 300 K | 300 K | 300 K | 123 K | 123 K | 10 K
Wavelength | 1064 nm | 1064 nm | 1064 nm | 1.5 - 2 mm | 1.5 - 2 mm | HF 1064 nm LF 1.5-2 mm
Substrate | Silica | Silica | Silica | Silicon | Silicon | HF Silica LF Sapphire
Beam radius (approx.) [cm] | 6 | 6 | 9 | 6.5 | 14 | HF 9 LF 7 (LG)
Coating thermal noise at 100 Hz [m/√Hz] | 1.3x10-20 | 6.5x10-21 (5.0x10-21) | 9x10-21 (5x10-21) | 2.3x10-21 | Optimistic 1.3x10-21 Pessimistic 5x10-21 | HF 3x10-21 LF 1.1x10-21
Coating loss [rad] | 3.6x10-4 (2.4x10-4) | 0.9x10-4 (0.6x10-4) | 2.4x10-4 (0.8x10-4) | 6.5x10-5 | Optimistic 5x10-5 Pessimistic 1.2x10-4 | HF 1.2x10-4 LF 1.3x10-4
Coating materials | SiO2 TiO2-Ta2O5 | SiO2 ?-Ta2O5 | SiO2 ?-Ta2O5 | SiO2/Al2O3 a-Si | SiO2/Al2O3 a-Si | SiO2/Al2O3/SiN ?-Ta2O5 a-Si ?
CE: Class. Quantum Grav. 34 (2017) 044001
ET: Class. Quantum Grav. 28 (2011) 094013 / Conceptual Design Doc.
aLIGO+: Phys. Rev. D 91 (2015) 062005 / LIGO-G1800514
Voyager: LIGO-T1400226-v9 / LIGO-G1801004
AdVirgo+ LIGO-G1800999

## Slide 7: Why do we think we can improve?
Most amorphous solids have loss angles in a limited range
(At least) two exception (in glasses):
  bulk silica at room temperature (low mechanical loss measured at room temperature)
  amorphous silicon grown at high temperature (low mechanical loss measured at low temperature)
What happens here?
Ta2O5/TiO2
SiO2 IBS
SiO2 disks
SiO2 bulk
Material loss angle
Zeitschrift für Physik B Condensed Matter. 101. 235-245
Phys. Rev. Lett. 113, 025503 (2014)
More in Frances Hellman’s talk

## Slide 8: Room temperature coatings (A+)
High temperature deposition of tantala did not show enough improvement
Two promising candidates: doping of tantala
Class. Quantum Grav. 35 (2018) 075001
15% Zirconia-doped-Tantala
Univ. of Strathclyde
LIGO-G1800585
Very slow deposition
high energy ions
Loss target
0.9x10-4
(0.6x10-4)
Annealed 750C
Refr. Index n = 2.12

## Slide 9: Room temperature coatings (A+)
Two promising candidates: doping of tantala
60% Titania-doped-Tantala
Univ. Colorado Fort Collins and Caltech
LIGO-G1800360
Steep frequency dependence
High optical absorption (contamination)
Loss target
0.9x10-4
(0.6x10-4)
Refr. Index n = 2.36

## Slide 10: What’s next?
Zr-doped-Ta:
  check dependency on concentration / deposition rate / method
  structural and modeling studies
  produce a multi-stack and do a direct measurement of thermal noise
Ti-doped-Ta:
  fix contamination and high optical absorption
  repeat measurements probing low frequencies, to confirm the slope
More in Kiran Prasai’s talk

## Slide 11: 123 K coatings (Voyager – C.E.)
Amorphous silicon deposited at high temperature is the best candidate
  High refractive index ~3.4
Low mechanical loss at low temperature. But at 123K?
  Measurements of loss at room temperature shows 𝜙 < 1x10-4 depending on deposition method
Optical absorptions still high, but improving
High-T deposited a-Si, loss
at low temperature (Berkeley)
deposition temperatures, Ts
annealed 350C
Loss target
5.5x10-5

## Slide 12: 123 K coatings (Voyager – C.E.)
Amorphous silicon deposited at high temperature is the best candidate
  High refractive index
Low mechanical loss at low temperature. But at 123K?
  Measurements of loss at room temperature shows 𝜙 < 1x10-4 depending on deposition method
Optical absorptions still high, but improving
High-T e-beam deposited a-Si (Berkeley)
Loss at room temperature (Caltech)
High-T IBS deposited a-Si,
Loss at room temperature (Strathclyde)
Blue: no post-deposition heat treatment
Red/pink: heat treated for 1hr at 400°C
Minimum loss: < 2 x 10-5 for deposition at 200°C + heat treatment at 400°C

## Slide 13: What’s next?
Measure mechanical loss angle of a-Si at 123 K
Improve optical absorptions
Structural measurements and modeling
Why the different behavior of mechanical loss with growth temperature?
Understand differences due to deposition method
More in Kiran Prasai’s talk
More in Frances Hellman’s talk

## Slide 14: Low temperature coatings (E.T.)
Amorphous silicon is a promising high index material
What about the low index material? Silica ≈ 5x10-4 at 10 K
Dependent on heat treatment
  In many cases annealing improves high temperature loss, but worsen low temperature loss
Al2O3 and SiN good low index candidates
Class. Quantum Grav. 31 (2014) 035019
From ET
conceptual design
Loss target
HF 1.2x10-4
LF 1.3x10-4

## Slide 15: Low temperature coatings (E.T.)
Magnetron sputtered Al2O3 (NRL) LIGO-G1800418
10-4
SiN CVD deposition
LIGO-G1800350
Amorphous silicon is a promising high index material
What about the low index material? Silica ≈ 5x10-4 at 10 K
Dependent on heat treatment
  In many cases annealing improves high temperature loss, but worsen low temperature loss
Al2O3 and SiN good low index candidates

## Slide 16: What’s next?
Further characterize Al2O3 and SiN mechanical loss
Improve optical absorption
Alumina shows improvement with growth temperature, similar to a-Si, dissimilar to Ta2O5

## Slide 17: Crystalline coatings
Promising candidate for 3rd generation
Low mechanical loss at room temperature (2x10-5)
Good optical absorption and good figure
Need to develop technology to scale up to large mirror size
G. Cole LIGO-G1800645
G. D. Cole, et al., Nature Photonics (2013)
AlGaAs room temperature: φRT < 4×10-5
AlGaAs cryogenic :
    φcryo < 5×10-6
Class. Quantum Grav. 32 035002 (2015)
More in Garret Cole’s and Manuel Marchio’s talks

## Slide 18: Structure and Modeling
Important to bridge mechanical loss, structural studies and modeling efforts
Use measured distributions to tune simulations and extract structural information
Reverse Monte Carlo + Energy minimization
Crucial: simulate the deposition process
Scientific Reports 6, 32170 (2016)
Measurements of pair distribution functions
K.Prasai LIGO-G1800872

## Slide 19: Outlook
Rate of progress significantly increased in the last few years
Promising candidates for A+ detector coatings (but we need a recipe very soon)
Amorphous silicon a promising candidate at mid and low T, but some more characterization are needed (and on-going)
Low temperature low index material? Some candidates (Al2O3, SiN)
Not one material good for all configurations
Other complementary directions:
Crystalline coatings Class. Quantum Grav. 32 035002 (2015)
Nano-layers LIGO-G1800300