| AUTHOR | DATE | REV | DCN NO. |
| --- | --- | --- | --- |
| BILLINGSLEY | 7/28/19 | V1 | E1900225 |

Applicable Documents

LIGO-D1900150 -v1		Mirror Blank Drawing, A+ Beamsplitter

MIL-G-174-B 			Glass, Optical

Requirements

Physical Dimensions 			per LIGO - D1900150

Clear Aperture 				Central 300 mm

Serial Number	Blanks shall be serialized as BSXX, where XX increments starting at 11

Material					Low Inclusion Fused Silica

Final shaping	Shaping shall be performed using a progression of grit size ending with a 320 or smaller grit tool.

Defect depth 				Maximum on any surface or corner is less than 0.5 mm

Index Homogeneity in central 110 mm	≤ 5.0 x 10-7 P-V

Index Homogeneity in clear aperture         ≤ 2.5 x 10-6 P-V

Birefringence				≤ 1 nm/cm within the clear aperture

≤ 5 nm/cm outside the clear aperture

Bubble and Inclusion Cross section 	Total ≤ 0.01 mm2/100cm3

Within the clear aperture 			Inclusions with a diameter of 10 m or less are not included

in the total.

Note all inclusions

Maximum inclusion diameter                      ≤ 0.1 mm

Striae 					Class 1

OH Content				≤ 1 ppm

| Specification | Method | Frequency of Inspection | Data Delivered |
| --- | --- | --- | --- |
| Physical Dimensions | Visual Inspection | 100% | Diameter Thickness |
| Serial number | Visual Inspection | 100% | Inspection Report included with Certification |
| Material | Process Control Material Certification | 100% | Inspection Report included with Certification |
| Defect depth | Visual Inspection | 100% | Hand sketch indicating location and dimensions |
| Homogeneity | Interferometric Measurement | 100% | Inspection Report included with Certification |
| Birefringence | MIL-G-174 Section 4.4.5 | 100% | Inspection Report included with Certification |
| Inclusions | Visual Inspection | 100% | Hand sketch indicating location and dimensions |
| Striae | MIL-G-174 Section 4.4.6, method 1 or 2 (in optical axis only) | 100% | Inspection Report included with Certification |
| OH content | Measurement | 100% | Inspection Report included with Certification |

Table 1: MEASUREMENT MATRIX: FREQUENCY AND METHOD